## Slide 1
Managing Corrosion- An Engineered Solution for Electronic and Mechanical Assemblies

## Slide 2
Cleaning and Unit Preparation
  DI Water Wash
      Some Hardware; Water Soluble Fluxes
  Aqueous Cleaning (water + chemicals)
      Optimal for Hardware; Most Fluxes including No Clean
  Solvent Cleaning
      Optimal for Hardware; RMA, Rosin, No Clean Fluxes, Oils
  Ultrasonic
      Increase Effectiveness of Standard Methods
  Mechanical – brushing & wiping

## Slide 3
Plasma Treatment and Surface Activation
  Dry Process
  Environmentally Friendly
      High Efficiency
      Reduced Waste Stream
  Removal of Contaminants
  Modify Surface Energy
      Increased Material Substrate Options
        Teflon, Plastics
  Increased Adhesion and Wettability

## Slide 4
Application Methodology
  CVD-Chemical Vapor Deposition
      Truly Conformal
  Dip coating
  Spray
  Multi faceted approach
      Increased Efficiency
  Layered approach
      Optimized Material Performance
        Example: Parylene with Urethane Overcoat

## Slide 5
Preferred Materials
Conformal Coating for Enhanced Corrosion Resistance

## Slide 6
Parylene
  Excellent Chemical Resistance
  Excellent Electrical and Mechanical Properties
  Protection from Corrosion
  Low Stress
  Thin Film

## Slide 7
EPOXY and URETHANE
    Great Material Compatibility
    Good to Excellent Chemical Resistance
      Ideal for harsh environments
      Moisture, Fluids, Corrosive Gases
    Good to Excellent Abrasion Resistance
    Thermo-mechanical Stability
    Tunable
      Mix Ratios, Additives/Fillers
      Greater Control of Physical and Electrical Properties

## Slide 8
Acrylics & Silicones
Low Stress
Good RF compatibility (Low Dielectric K)
      Ideal material for antenna
Reduced Process Complexity
Easily Reworked /repairable

## Slide 9
Nano Technology
Inorganic Coatings (ASG)
      High Operating Temperature Limits
Thin Film

## Slide 10
 |  |  |  |  | Rating Scale 1 (Highest) to 4 |  | 
 | Acrylic | Polyurethane | Epoxy | Silicone | Parylene (XY) |  | 
 | (AR) | (UR) | (ER) | (SR) | C | D | N
Humidity Resistance | 2 | 1 | 2 | 1 | 2 | 2 | 1
Humidity Resistance (Extended Periods) | 2 | 1 | 3 | 2 | 2 | 2 | 1
Abrasion Resistance | 3 | 2 | 1 | 4 | 1 | 1 | 1
Mechanical Strength | 3 | 1 | 1 | 2 | 1 | 1 | 1
Temperature Resistance | 2 | 3 | 3 | 1 | 2 | 2 | 1
Acid Resistance | 3 | 1 | 1 | 2 | 1 | 1 | 1
Alkali Resistance | 3 | 1 | 1 | 2 | 1 | 1 | 1
Organic Solvent Resistance | 4 | 1 | 1 | 2 | 1 | 1 | 1
Dielectric Constant (1MHz @ 23°C) | 2.2 - 3.2 | 4.2- 5.2 | 3.3 - 4.0 | 2.6 - 3.0 | 3.15 | 2.84 | 2.65
Outgassing | 3 | 2 | 3 | 4 | 1 | 1 | 1
Electrical Impedance | 2 | 4 | 3 | 2 | - | - | -
Optical Clarity | 4 | 3 | 1 | 2 | 2 | 2 | 2
Electrical Insulation | 1-2 | 1-2 | 1-2 | 2 | 2 | 2 | 1
Reworkability | 1 | 3 | 3 | 2 | 4 | 4 | 4
VOC’s | 1-3 | 2-3 | 2-3 | 1-2 | 1 | 1 | 1
Thermal Stability | 1-2 | 2 | 2 | 1-2 | 1 | 1 | 1
Thermal Conductivity | 2-3 | 1-3 | 1-3 | 2-3 | 3 | 3 | 3
Adhesion | 2-3 | 1-2 | 1-2 | 1-3 | 2 | 2 | 2
Material Selection Table

## Slide 11
EMI RFI Shielding

## Slide 12
FORM-IN-PLACE conductive gaskets offer effective EMI RFI shielding, ESD control and environmental seal.
Multi-Axis CNC dispensing for precise, repeatable, high reliability sealing.
Capable of mitigating Internally or Externally radiated interference.
Can be applied to nearly all conductive surfaces where a seal is required including conductive coated or metallized composites.
FIPG (Form-In-Place Gasket)

## Slide 13: Conductive Coatings
Coatings are typically applied to hardware or electronics through spray application or CNC dispensing.
Excellent EMI RFI shielding
High Attenuation
Adaptable material properties

## Slide 14
Nano Technology
Optically Clear Material Solutions Available
        Ideal for Lighting Solutions (LED)
        Can Replace ITO (Indium Tin Oxide)
Applied Easily Using Conventional Methodologies
        Spray
        Dip